ANTI-CORROSIVE APPLICATION PROCEDURE.

1. INTRODUCTION

Nyati Paints “Anti-corrosive” paint is a water-based, non-toxic, non-flammable coating.The product is a semi-gloss, quick-drying, self-etch, anti-corrosive, barrier coat which is highly resistant to chemical attack and ultra violet light. In essence, a primer with top coat qualities.

2. SURFACE PREPERATION

- The most important process in any paint application operation is the surface preparation to ensure bonding to the substrate.

- Substrate to be painted must be prepared to a water break free surfaces, therefore a galv-wash needs to be used. (Nyati Paints Ezi-Clean). Ezi-Clean is a water-base degreaser which contains some Phosphoric acid to etch the surface and remove oil and grease. The entire area to be coated must be washed and scrubbed, then rinsed off with clean running water. Allow at least 1 hour’s drying time.

- Remove all loose rust flakes and orange rust with a wire brush, sandpaper, sandblast, etc. Making sure that the surface is oil and grease free by washing it with Nyati Paints Ezi-Clean and rinse with clean water. Do NOT use thinners, turps or any solvent to remove oil or grease, as solvent is oil based and will still leave a thin layer of oil on the surface.

3. APLICATION

- Paint is easily applied by brush, roller, or airless spray.

The following should be ensured before paint application commences:

- Being a water base paint, surfaces to be painted must not be too cold or too hot. The surface temperature of the item to be painted must be between 10°C and 30°C. As a guideline if, under prevailing site conditions, you can place your bare hand on the item to be painted for longer than 1 minute, then painting may proceed.

- If in doubt, take a measurement of the humidity and, if it is within the accepted limits (MAX.85%), proceed painting. Under prevailing site conditions, the practical test used is to take a damp cloth and press it firmly on the area to be painted. If the resultant damp patch disappears within 15 minutes, then painting may commence.

3.4	Remove all dust by wiping the surface of the item to be painted with a damp cloth. Do NOT 	blow dust off, as it will hang in the air and, after painting, will re-settle on the wet paint.

3.5	Remove any dew from items to be painted with a clean dry cloth and allow to dry properly 	before applying top coats.

  - Prepare for painting away from the direction of the wind, and dust caused by dirt roads.

3.7	Do NOT dilute the paint.

4.	APPLYING THE SECOND COAT 		(Final DFT 70 µ min)

4.1	Upon completion of the first coat, the drying time between that and the final coat, must be       	at least 1.5 hours. During winter, a minimum of 2 hours must be allowed for.

4.2	Allow 8 hours to a day for the paint to cure properly.

4.3	For high risk areas, (Coastal, salt spray; and Desert, sandstorm) a third coat, as well as a final Aquanamel-clear coat is recommended, to give a final paint thickness of 120-150 micron.

5.	HIGH GLOSS ENAMEL EMULSION PAINT (AQUANAMEL CLEAR)

5.1	Should a Customer request a high gloss finish, this can be applied as an additional final clear coat.

5.2	The clear gloss coat must be applied after allowing a total drying time of 4 hours after the 2nd     or final anti-corrosive coating is applied.

6.	TOUCH UP OF DAMAGED AREAS

6.1	Scratches and abrasions sustained during rigging and transport must be sanded down to at least 25mm around the damaged area, and the area made good with Nyati anti-corrosive paint to the same original thickness.

6.2	If a gloss coat was specified, the clear gloss must also be applied to all touched up areas.

7.	CLEANING OF MATERIALS AND EQUIPMENT

7.1	Cleaning before final site inspection: Dirt marks on paint are to be removed with soap and water, NOT solvent.

7.2	Clean all equipment with soap and water. And rinse with clean running water, allow the equipment to dry before using it again.

8.	SEE THE COMPANY SPESIFICATION AND MATERIAL SAFETY DATA SHEETS FOR TEQNICAL DATA.